## Slide 1: Biofabrication and its in\xc2\xa0vitro toxicity mechanism of silver nanoparticles using Bruguiera cylindrica leaf extract\r\n\r\n

## Slide 2: MAIN-TITLE
Biofabrication and its in\xc2\xa0vitro toxicity mechanism of silver nanoparticles using Bruguiera cylindrica leaf extract\r\n\r\n

## Slide 3: HIGHLIGHTS
\r\n\r\n\r\n \r\n \r\n \r\n \r\n \r\n \r\n AgNPs were synthesized using Bruguiera cylindrica extract as reducing agent
\r\n\r\n\r\n \r\n \r\n \r\n Green synthesis of AgNPs is a simple, economic and by eco-friendly approach
\r\n\r\n\r\n \r\n \r\n \r\n Hexagonal AgNPs were derived
\r\n\r\n\r\n \r\n \r\n \r\n AgNPs shows good cytotoxic effect against MCF-7 breast cancer cell lines
\r\n\r\n\r\n \r\n \r\n \r\n \r\n \r\n\r\n

## Slide 4: KEYPHRASES
\r\n\r\nGreen synthesis\r\n\r\n\r\n\r\n\r\n Bruguiera cylindrica\r\n\r\n\r\n\r\n\r\n \r\n\r\nSurface plasmon resonance\r\n\r\nCell line culture\r\n\r\n

## Slide 5: ABSTRACT
\r\n\r\n\r\n \r\n \r\n Silver nanoparticles (AgNPs) were synthesized using Bruguiera cylindrica (B
cylindrica) leaf extract, the extract was acted as a reducing and stabilizing agent
The X-ray diffraction (XRD) analysis shows that the particles are face centered cubic (fcc) structure and average size of AgNPs was found at 16\xc2\xa0nm

## Slide 6: INTRODUCTION
\r\n\r\nNanotechnology is the engineering of functional systems at the nano scale level with multi-disciplinary areas of applied science and engineering
But they are having some limitations in their synthesis and application aspects [6,7]
The present study has aimed to synthesis, characterization and cytotoxic effect of green AgNPs using B
cylindrica leaf extract
\r\n\r\nMatured fresh leaves of B
cylindrica were collected from Pichavaram Mangrove forest, Tamil Nadu, India
The fully dried leaves were powdered with a sterile electric blender
2\xc2\xa0ml of B
cylindrica leaf extract was added to 20\xc2\xa0ml of AgNO3 solution and kept at room temperature [17]
\r\n\r\nThe absorption spectrum of the reaction mixture was recorded at room temperature using UV\xe2\x80\x93vis spectrophotometer (Hitachi-U-2001) from 300 to 800\xc2\xa0\xc2\xa0nm at 1\xc2\xa0nm resolution for detection of AgNPs formation
The size distribution and shape of NPs were estimated on the basis of TEM micrographs
The percentage of viability was calculated by using the following formula,\r\n \r\n \r\n \r\n Percentage\r\n \r\n of\r\n \r\n viability\r\n =\r\n \r\n \r\n Sample\r\n \r\n absorbance\r\n \r\n \r\n (\r\n AgNPs\r\n )\r\n \r\n \r\n \r\n Control\r\n \r\n absorbance\r\n \r\n \r\n (\r\n untreated\r\n )\r\n \r\n \r\n \r\n \xc3\x97\r\n 100\r\n \r\n \r\n \r\n \r\n \r\n\r\n

## Slide 7: CONCLUSION
\r\n\r\nTo conclude from this study, the synthesis, characterization and cytotoxic effect against MCF-7 cell lines of biosynthesized AgNPs was performed using B
cylindrica leaf extract as stabilizer and reductant

## Slide 8: ACKNOWLEDGMENTS
\r\n\r\nWe are grateful to the Management of J
J
College of Arts & Science, Pudukkottai, Tamil Nadu, India for providing a Research grant (KVET-RG-2014-BT03) by Karpaga Vinayaga Educational Trust for conduct this work